Homework #4

- GaAs has an Longitudinal Optical Phonon energy of 36 meV, and we usually take this energy to mean the Optical Phonon near k=0.

- If you modeled GaAs as a linear diatomic chain with equal spring constants between each atom, what would be the spring constant K in Nm-1?

- Using the K from (a), what would expect for the Optical Phonon energies for InAs, InP, and GaP?

- Find the LO Phonon energy values for the three above materials.  How do they compare to your results in (b)?

- The conduction band electron effective masses for Si and Ge are given below:

|  | Ge (m*/m) | Si (m*/m) |
| --- | --- | --- |
| m*l | 1.588 | 0.916 |
| m*t | 0.08152 | 0.1905 |

Draw, best you can, or plot using a 3D plotting program, the constant energy surfaces for Si and Ge conduction band electrons.

- Using the results from our discussion of Phonons in crystals, plot the lattice vibration waves in position, at a fixed t, for Acoustic and Optical Phonons at k=0, and k=π/a.  Describe the relative motion of the atoms for each of these four cases.

- For GaAs, calculate the amplitude (in m) of the acoustic phonon vibrational wave in a 1mm cube.